## Slide 1
Developing Pr0.6Sr0.4Mn0.2Fe0.8O3-δ Solid Oxide Electrolysis
Cells to Support NASA’s Future Manned Missions to Mars
As NASA looks towards sending manned missions to Mars, a reliable oxygen source, as well as a returning fuel source, needs to be refined. Such resources are difficult to transport, which require the need for producing these resources on-site once landed on Mars. Further research is critical to NASA’s Human Exploration & Operations Mission Directorate regarding the In-Situ Resource Utilization (ISRU) program.
Introduction
What are solid oxide electrolysis cells?
  Solid oxide electrolysis cells (SOEC) are
  cells that convert electricity into a chemical
  reaction. They operate at high temperatures
  and are a clean way to produce oxygen
  gas from carbon dioxide.
Comprised of an electrolyte and electrodes
Triggers the reaction of 2CO2  2CO + O2
Background
PrSrMnFe SOEC show high performance under CO2 atmospheric conditions under high temperatures, therefore, it is a viable catalyst for future SOEC manufacturing.
Conclusion
References:
  [1] Park, K. Y., Lee, T., Wang, W., Li, H., & Chen, F. (2023).
  High-performance Ruddlesden–Popper perovskite oxide with in situ exsolved nanoparticles for direct CO 2 electrolysis. Journal of Materials Chemistry A, 11(39), 21354-21364.
  Sol-gel method: Cell assembly:
  Cell fabrication:
Colloidal solution; evaporating at 80°C
Combustion at 400°C
Final ceramic product; incinerated at 1100°C
Gel formation
Xerogel formation
Results
Performance Testing
Au current collectors
LaSrCoFe
electrode
LaSrGaMg
electrolyte
PrSrMnFe
electrode
X-Ray Diffraction
Step 1: 30°C  575°C
Step 2: 575°C  800°C
Step 3: 800°C  1000°C
Thermogravimetric Analysis
Methods
  Eva Godwin, Ramin Babazadeh Dizaj, Fanglin (Frank) Chen, PhD
In performance testing, cell was probed in a CO2 atmosphere and heated. Electrochemical impedance spectroscopy and voltage vs. current density plots were created from temperature ranges of 600°C to 800°C.
XRD, TGA, and GC plots were created to determine material properties.
Gas Chromatography
Electrolyte tape casting
Electrode ink preparation
Screen printing electrode
Coat electrodes with Au paste; mount to ceramic tube with Ag paste
Seal with ceramic paste
NASA’s MOXIE: Mars Oxygen In-Situ Resource Utilization Experiment
Voltage behavior and CO content in the product gas of the single cell at 800 °C with applied current densities of 0.1, 0.2, and 0.3 A cm-2
Department of Mechanical Engineering, University of South Carolina, Columbia, SC
2θ (°)
Notes: the goal of our project was to address the issue of the lack of oxygen on mars's surface. oxygen is needed for ---------- and transporting is difficult, especially for prolonged stay